Specification for Recycled Polypropylene:
rPP Flake – Non-food contact – Grade C

| Background |  |  |
| --- | --- | --- |
| Indicative processing | To meet the Mandatory Criteria in this specification, plastic will typically need to go through the following processing steps according to its condition and source: Condition; Source; Processing steps. Used; Mixed stream (co-mingled); - Multiple sorting processes – eg manual, optical, density, magnetic - Washing and drying - Size reduction (shredding / cutting / grinding). Single stream; - Targeted sorting as required - Washing and drying - Size reduction (shredding / cutting / grinding). Unused; Mixed or single stream; - Targeted sorting as required - Size reduction (shredding / cutting / grinding). Plastic sourced from automotive, electronic, construction, or chemical storage container waste is not suitable for this specification. |
| Indicative uses | Plastic processed in accordance with this specification is suitable for manufacture via repelletising, blow moulding, injection moulding, extrusion or fibre spinning into new non-food contact items such as automotive parts including dashboards and door panels, furniture such as chairs, stools and plastic shelving, rigid storage containers such as stackable bins, and woven shopping bags, shipping pallets and crates. |  |
| Mandatory Criteria Waste plastic processed to this specification must comply with the following mandatory criteria. Relevant testing methodologies are noted as a guide only and are not mandatory. |  |  |
| Criteria |  | Relevant testing methodologies |
| Polymer | Polypropylene (PP) |  |
| Prohibited Content | Any substance or material, including components or additives in the plastic, which: - meets the definition of ‘hazardous waste’ in the Hazardous Waste (Regulation of Exports and Imports) Act 1989, or - is prohibited from export under Schedule 6 or 7 of the Industrial Chemicals Environmental Management (Register) Instrument 2022. |  |
| Allowable Contaminants | Up to a combined total of 5% of the following contaminants only, not exceeding their individual subtotals: - Other polyolefin polymers (LDPE, LLDPE, HDPE) = up to a subtotal of 5% - Other contaminants as agreed with importers in writing (see Additional Criteria) = up to a subtotal of 2% *Contaminant means any substance or material that is not PP (excluding Prohibited Content, moisture and any substances inherent in the PP plastic such as stabilisers, dyes and plasticisers). Examples include other plastics, metals, glass, paper and wood. *Thresholds are given as a percentage of total weight. | - Annex A of 18263-2:2015 - ISO 1183-1:2025 - ISO 11357-3:2025 - Annex A of EN 15347-1:2024 - Annex A of EN 15344:2025 |
| Form | Flake measuring 5-20 mm (with any specific dimensions and/or flake size distribution within that bracket to be agreed with importers in writing – see Additional Criteria). *Flake means small, typically flat, irregularly shaped pieces of material formed by shredding, cutting or grinding larger rigid plastic items during the recycling process. | - Annex A of EN 15348:2024 |
| Packaging for export | Bagged and packed in sealed shipping containers. |  |
| Additional Properties Additional properties of the plastic processed to this specification may be agreed below with individual importers from time to time, provided the properties are consistent with the Mandatory Criteria. Relevant testing methodologies are noted as a guide only. |  |  |
| Additional agreed properties |  | Relevant testing methodologies |
| Colour |  | Visual inspection |
| Specific contaminants |  | - ISO 1183-1:2025 - ISO 11357-3:2025 - Annex A of EN 15347-1:2024 - Annex A of EN 15344:2025 |
| Specific flake dimensions |  | - Annex A of EN 15348:2024 |
| Flake size distribution |  |  |
| Fines |  |  |
| Bulk density |  | - Annex B of ISO 12418-2:2012 - ISO 60:2023 |
| Melting temp range |  | - ISO 11357-3:2025 |
| Moisture |  | - Annex B of EN 15348:2024 |
| Other |  |  |
| Agreed between: |  |  |
| Date: |  |  |